Technical Note

Roseburg EWP Products Treated with Hi-Clear II™                    January 30, 2018

Roseburg Forest Products RigidLam®Laminated Veneer Lumber (LVL) and RFPI®Joist products may be pressure treated with the Hi-Clear II preservative system produced by Permapost Products Co. at their facilities located in Hillsboro, Oregon.

Testing performed by APA-The Engineered Wood Association indicates that the Permapost Hi-Clear II treatment does not adversely affect the strength or stiffness properties of Roseburg LVL or I-joists.

Therefore, Roseburg Forest Products LVL and I-joist products treated with Permapost Hi-Clear II preservative are acceptable for use in above-ground, interior or covered exterior, dry-use environments.  The LVL and I-joists, not the treatment, will be covered by Roseburg’s Engineered Wood Products and Performance Warranty.

Roseburg makes no statement regarding the quality or efficacy of the Hi-Clear II treatment.  It is the responsibility of the end user of any treated material to be familiar with the appropriate material safety data sheets and handling instructions associated with the treated product.